PRODUCT DATA SHEET

UMC-BEN 11

BENTONITE POWDER API SEC 11

DESCRIPTION:

UMC-BEN 11 is a sodium montmorillonite bentonite conforming with API 13 A Sec 11.

UMC-BEN 11 is a viscosifier and fluid loss reducer agent for all types of water based systems.

PHYSICAL PROPERTIES:

| Appearance | Light brown to grey free flowing powder |
| --- | --- |
| Type | Sodium montmorillonite confirms With API 13A Sec 11 |
| Bulk density | 795-805 kg/m³ |
| Density | 2.5 g/cm³ |
| Ph (5% suspension) | 9 |

APPLICATIONS:

UMC-BEN11  is used to increase viscosity and reduce fluid loss in water base drilling fluids. It is a cost-effective means of achieving viscosity, fluid-loss control and filter-cake

quality  in freshwater and seawater muds. In salt water muds it should be pre-hydrated in freshwater to achieve the maximum yield prior to circulating the substances to the mud system.

Bentonite usage depends on type of mud systems and operational requirements. In spud mud the dosage  ranges from 15-25 ppb to prepare high viscous muds, while in bentonite/salt gel system for upperhole section it can used 10-15ppb. In polymer and dispersed systems the dosage  ranges from 5-12ppb where in all cases the UMC-BEN 11 should be pre-hydrated in fresh water and to be mixed through the hopper.

PERFORMANCE SPECIFICATIONS:

1.Viscometer dial reading @ 600 rpm – min 30

2.Yield point/plastic viscosity ratio – max 6

3. Filtrate volume –max 16 ml

4. Residue greater than 75 micrometers –max 2.5 % wt

5.Moisture – max 12% wt

TOXICITY & HANDLING:

Bioassay information is available upon request. Handle as an industrial chemical, wearing protective equipment and observing the precautions as described on the transportation and Material Safety Data Sheet (MSDS)

PACKING:

UMC-BEN 11 is packed in 25 Kg, 50 Kg, 1000 Kg bags.